Last Updated: 23.04.2018

Product Code: I00812

SAROL 04P (DUSTROL) is a blend of highly refined, solvent neutral, paraffinic mineral oil and orange/honey oil reodorant.

APPLICATION

Use as received in a wide range of applications where a non-additive mineral oil is required.

When sprayed it is also suitable for use as an effective dust suppressant.

N.B.– although not inherently hazardous, the use of good industrial practice regarding personal protection to limit exposure is recommended when used for this purpose.

BENEFITS

- Excellent lubricity properties make it suitable for a wide range of uses

- The product has excellent stability over long periods of application and will not polymerize

- Capable of blending easily with additives if required

- Can be used as an excellent solvent oil

TYPICAL PROPERTIES

Colour & Appearance:			Pale, clear liquid

Odour:					Orange/Honey

Density @ 15.60C:			0.814-0.828

Closed Flash Point:			1330C

Kinematic Viscosity @ 400C:		3.5 - 4.5 cSt

Boiling Point:				>1000C

HEALTH & SAFETY

This product has been manufactured to the highest standards and when used for the purpose recommended is unlikely to present any significant health hazards. A Material Safety Data Sheet is available.

Indicated data are approximate values and are subject to the usual commercial fluctuations.  All information correct at time of going to press to the best of our knowledge. This information may be subject to change without notification due to continual product research and development.